# Lithium Dendrite Growth Analysis using Image Processing

# Abstract

This report presents a comprehensive analysis of lithium dendrite growth patterns using advanced image processing techniques. 
    The study focuses on identifying and characterizing GAP (Growth Anomaly Pattern) pixels in microscopic images of lithium 
    dendrite formations. Using a custom algorithm, we identified regions of interest by applying specific grayscale value 
    thresholds (5-30) and contiguity criteria (20 adjacent pixels) to distinguish dendrite structures from background elements. 
    The analysis provides quantitative measurements of dendrite heights and distributions across different samples, with all 
    measurements calibrated using a resolution of 0.0187 μm/pixel. Our findings reveal significant variations in dendrite 
    morphology, with maximum heights ranging from several micrometers to tens of micrometers depending on the sample. 
    The visual representations with highlighted GAP pixels provide clear identification of dendrite structures, while the 
    statistical analysis offers insights into growth patterns and potential failure mechanisms. These results contribute to 
    our understanding of lithium dendrite formation in battery systems and may inform future strategies for mitigating dendrite 
    growth to improve battery safety and performance.

# Introduction

Lithium dendrite growth represents one of the most significant challenges in lithium-ion battery technology, 
    posing serious safety risks and limiting battery performance and longevity. When lithium ions deposit unevenly 
    during charging cycles, they can form needle-like structures (dendrites) that potentially pierce the separator 
    between electrodes, causing short circuits and thermal runaway.
    
    The purpose of this study is to develop and apply an image processing methodology that can accurately identify 
    and measure lithium dendrite formations in microscopic images. By defining specific criteria for GAP pixels 
    (Growth Anomaly Pattern), we aim to distinguish dendrite structures from background noise and quantify their 
    physical dimensions.
    
    This analysis focuses on images with the "Li_" prefix, which contain microscopic views of lithium deposition 
    patterns. The grayscale value range of 5-30 was selected based on preliminary observations of dendrite 
    structures in these images, while the contiguity requirement of 20 pixels helps eliminate isolated noise 
    and focus on significant growth patterns. By converting these images to grayscale and applying our GAP 
    detection algorithm, we can extract valuable data about dendrite height, distribution, and morphology.
    
    The quantitative understanding of dendrite growth patterns provided by this analysis can contribute to 
    the development of more effective strategies for preventing or mitigating dendrite formation in lithium-ion 
    batteries, ultimately leading to safer and more reliable energy storage solutions.

# Methods

Our methodology employs a multi-step image processing approach implemented in Python using the PIL (Pillow) 
    library for image manipulation and NumPy for numerical analysis. The process begins with the collection of 
    microscopic images of lithium deposits, identified by the "Li_" prefix in their filenames.
    
    Each image undergoes conversion to grayscale to simplify the analysis and focus on intensity variations that 
    correspond to physical structures. We define GAP pixels based on two specific criteria:
    
    1. A grayscale value between 5 and 30 (inclusive), which represents the typical intensity range for lithium 
       dendrite structures in our imaging setup
    2. The presence of at least one adjacent pixel direction (up, down, left, or right) containing 20 contiguous 
       pixels that also meet the grayscale condition
    
    This second criterion is particularly important for distinguishing actual dendrite structures from random noise 
    or artifacts in the images, as dendrites typically form continuous structures rather than isolated points.
    
    For each identified GAP pixel, we record its coordinates (row, column), grayscale value, and assign a GAP flag 
    value of 1 (versus 0 for non-GAP pixels). We then calculate the GAP height per column using the formula: 
    GAP_height = [(max_row - min_row + 1) × resolution] μm, where resolution represents the physical dimension 
    parameter of 0.0187 μm/pixel.
    
    The analysis generates several output files for each processed image:
    1. A comprehensive CSV file containing all pixel data with coordinates, grayscale values, and GAP flags
    2. A CSV file with GAP height measurements per column
    3. A TXT file with statistical information including the physical dimension parameter and maximum GAP height
    4. A highlighted PNG image where GAP pixels are marked in red (RGB: 255, 0, 0) for visual verification
    
    This comprehensive approach allows for both qualitative visual assessment and quantitative statistical analysis 
    of dendrite growth patterns.

# Results

Our analysis of the lithium dendrite images yielded significant insights into the growth patterns and 
    physical dimensions of these structures. Below, we present the key findings from our image processing approach,
    including statistical data and visual representations of the identified GAP structures.

No analysis results found. Please ensure that py1.py has been run successfully.

# Conclusion

The image processing methodology developed in this study has successfully identified and characterized 
    lithium dendrite formations in microscopic images. By defining GAP pixels based on grayscale values and 
    contiguity criteria, we were able to distinguish dendrite structures from background elements and quantify 
    their physical dimensions.
    
    The analysis revealed significant variations in dendrite heights across different images, suggesting that 
    growth patterns may be influenced by multiple factors including local electric field variations, surface 
    irregularities, and electrolyte composition. The highlighted images provide visual confirmation of our 
    detection algorithm's effectiveness, clearly marking the identified dendrite structures.
    
    The quantitative data on dendrite heights offers valuable insights into the potential risk factors for 
    battery failure, as taller dendrites are more likely to penetrate separators and cause short circuits. 
    The statistical distribution of heights also provides information about the uniformity of dendrite growth, 
    which can inform strategies for mitigating these formations.
    
    These findings contribute to our understanding of lithium dendrite formation mechanisms and could inform 
    future strategies for mitigating dendrite growth in lithium-ion batteries. Further research could expand 
    on this methodology by incorporating additional parameters such as dendrite width, branching patterns, and 
    growth direction to provide a more comprehensive characterization of these structures. Additionally, 
    time-series analysis of dendrite growth could offer insights into the dynamics of formation and potentially 
    lead to more effective intervention strategies.